**EC Declaration of Performance**

1. Unique identification code of the product-type:

**Forte**

**Unique batch code is on packaging**

2. Intended use/es:

**General Purpose rendering / plastering mortar.**

3. Manufacturer:

**Lime Green Products Ltd**

**Coates Kilns**

**Stretton Road**

**Much Wenlock**

**Shropshire**

**TF13 6DG**

4. Authorised representative:

**N/A**

5. System/s of AVCP:

**System 4**

6a. Harmonised standard:

**EN998-1:2010**

6b. European Assessment Document:

**N/A**

7. Declared Performance

|  |
| --- |
| CE |
| Lime Green Products Ltd, Coates Kilns, Stretton Road, Much Wenlock, Shropshire, TF13 6DG  16 |
| **Forte**  **EN 998–1:2010**  **Factory Made General Purpose Rendering and plastering mortar for internal and external use**  **Reaction to fire:** Class A1  **Strength Class**  CSIII  **Adhesion and fracture pattern:** >0.15 FP: B  **Capillary Water absorption:** W0  **Water vapour Permeability coefficient.** µ ≤15  **Mean thermal conductivity λ10,dry [W/mK]** 0.82  **Durability:** (against freeze/thaw)**:** evaluation based on provisions valid in the  intended place of use of the mortar |

The performance of the product identified above is in conformity with the set of declared performance/s. This declaration of performance is issued, in accordance with Regulation (EU) No 305/2011, under the sole responsibility of the manufacturer identified above.

**Date 2/8/16**

**Signed**

J Ayres – Director