**EC Declaration of Performance**

**Lime Green Product Ltd**

**Coates Kilns**

**Stretton Road**

**Much Wenlock**

**TF13 6DG**

Declares that the product **Lime Green Ashlar Mortar,** described in the product datasheet, is manufactured at the above address**,** has undergone relevant Initial Type Testing and complies with the requirements of annexe ZA1 of EN BS 998:2 2010.

**Lime Green Ashlar Mortar** is made under Factory Production Control at the above address according to Annexe ZA2 of EN BS 998 -2 and complies with the requirements of CE marking.

|  |
| --- |
| CE |
| **Lime Green Products Ltd**  **Coates Kilns, Stretton Road, Much Wenlock, TF13 6DG**  **13** |
| **EN 998–2**  **Prescribed General Purpose masonry mortar for external use**  **Proportion of Constituents (by volume):**  Natural Hydraulic Lime: 1 Part  Aggregates: 2 Parts  **Contents of chloride:** NPD  **Water absorption:** 1.5 kg/(m2.min0.5)  **Water vapour permeability:** μ5 / 20  **Reaction to fire:** Class A1  **Thermal Conductivity:** (λ10,dry) *P* =50%: 0.47 W/mK  *P* =90%:0.54W/mK  **Durability (against freeze-thaw):** evaluation based on provisions valid in the intended place of use of the mortar. |



Signed:

Name: James Ayres

Position: Director

Date: 22/2/2013