|  |
| --- |
| **CE**  **EC Declaration of Performance** |
| Lime Green Products Ltd, Coates Kilns, Stretton Road, Much Wenlock, Shropshire, TF13 6DG  15 |
| **Finish WP**  **EN 998–1:2010**  **Factory Made Coloured Rendering Mortar (CR) for external use**  **Reaction to fire:** Class B1  **Strength Class**  CSII  **Adhesion:** >0.08 (woodfibre)  **Capillary Water absorption:** W2  **Water vapour Permeability coefficient.** µ ≤10  **Thermal conductivity λ10,dry [W/mK] *P=50%*** 0.47  ***P= 90%*** 0.54  **Durability (against freeze/thaw):** evaluation based on provisions valid in the  intended place of use of the mortar |

**Date** 22/1/15

**Signed**

J Ayres – Director