|  |
| --- |
| **CE**  **EC Declaration of Performance** |
| Lime Green Products Ltd, Coates Kilns, Stretton Road, Much Wenlock, Shropshire, TF13 6DG  13 |
| **EN 998–1:2010**  **General purpose (GP) rendering mortar for external use**  **Reaction to fire:** Class A 1  **Adhesion:** 0.9N/mm2 FP: b  **Capillary Water absorption:** W0  **Water vapour Permeability coefficient.** ≤15  **Thermal conductivity λ10,dry [W/mK] *P=50%*** 0.67  ***P= 90%*** 0.76    **Durability:** (against freeze/thaw)**:** evaluation based on provisions valid in the  intended place of use of the mortar |

**Lime Green Natural Stipple**

**Date** 28/8/13

**Signed**

J Ayres – Director