EC Declaration of Performance

Lime Green Products Ltd, Coates Kilns, Stretton Road, Much Wenlock, Shropshire, TF13 6DG 13

EN 998–1:2010 General purpose (GP) rendering mortar for external use Reaction to fire: Class A 1 Adhesion: 0.9 N/mm2 FP: b Capillary Water absorption: W0 Water vapour Permeability coefficient. ≤15 Thermal conductivity λ10,dry [W/mK] P=50% 0.67 P= 90% 0.76 Durability: (against freeze/thaw): evaluation based on provisions valid in the intended place of use of the mortar

Lime Green Natural Stipple

Date		28/8/13

Signed

J Ayres – Director