## Lime Green: Warmshell Internal IWI System

## Guideline product specification

• Manufacturer: Lime Green Products Ltd

 - Web: www.lime-green.co.uk

 - Email: sales@lime-green.co.uk

 - Tel: +44 (0)1952 728 611

 - Fax: +44 (0)1952 728 361

 - Address: Coates Kilns, Stretton Road, Much Wenlock, TF13 6DG

• Product reference: Lime Green Warmshell IWI System

• Substrate: Existing / New masonry of brickwork / stonework

* Substrate to be dry and sound before work commences.
* Preparation: Not required / re-point externally with Lime Green mortar/ remove existing impervious coatings / make good gutters and rainwater goods / install French drain.
* Levelling coat: Not required – existing unpainted lime plaster / Lime Green Duro Natural. Achieve a flatness of +- 10mm under a 2m rule

• Insulation

* Warmshell Woodfibre Boards
* Thickness 40mm / 60mm / other
* Fixing method : Apply full bed of Warmshell Board Adhesive with a 10mm notched trowel to the back of the board and fit immediately. Supplementary hammer fixings as required : 1/4/5/other per board. Type …

• Plaster

* Plaster re-enforcement mesh: Lime Green 454 mesh
* Plaster : Lime Green Solo applied in 2 passes, total 10mm thick.

• Paint

* Allow to fully dry before painting. Use mineral, breathable paints.

Fixings for surface mounted objects: Ejot Spiral / Ejot Iso Dart / Ejot Iso Bar

*Please consult Lime Green for assistance with detailing or a custom specification.*

This information is prepared for indicative purposes only.  Lime Green Products Ltd shall not be liable for the consequences of any use of this information for any purpose other than that for which it was prepared and accepts no duty of care in relation to the same.

21/7/20