## Lime Green Warmshell

## External Wall Insulation System

## Guideline spec for timber frame; two coat render system and woodfibre boards

• Manufacturer: Lime Green Products Ltd

- Web: 	www.lime-green.co.uk

- Email: 	sales@lime-green.co.uk

- Tel: 	+44 (0)1952 728 611

- Fax: 	+44 (0)1952 728 361

- Address: 	Coates Kilns, Stretton Road, Much Wenlock, TF13 6DG

• Product reference: Lime Green Warmshell EWI System

• Substrate: New timber frame

- Levelling coat: Not required

• Insulation

- Beneath DPC: XPS slab / Jablite Bastherm /Not applicable

- Thickness: ___ mm

- Fixing: WT / WTS

- Above DPC: Lime green Woodfibre board

- Thickness: ___ mm

- Fixing: STR-H

- Baserail; Aluminium with bead

  - Width: __mm

• Beads & Sealing

- Reveals & soffit: Frameseal 15mm

- Junctions between insulation and other material: Compriband 600

- Corners etc: hidden mesh wing bead / PVC corner bead

- Steico Fix system for cills: depth according to board thickness

• Render

- Reinforcement mesh: Lime Green 660 mesh

- Undercoats

  - On XPS: Lime Green Prepbond WP

  - On Woodfibre: Lime Green Prepbond WP

- Finish Coat: Lime Green Finish WP

  - Colour: 020 / 021 / ___ etc, tbc.

  - Texture: F / M / tbc.

  - Style: Sponge / Scraped / Cast / tbc.

• Accessories:  Vertical movement joints / horizontal full system movement joint /  roof ventilation plate / special coping / system stop ends / Compriband

Please consult Lime Green for assistance with detailing or a custom specification.